## Slide 1
PVRD 3D Internal Update
Mar 25th, 2019

## Slide 2: Ellipsometry
Results over full surface
Results:
  Thickness across sample
  Complex index of refraction
10% in thickness variation of SiNx layer position tracking required
Ellipsometry results
Sample summary | AC1 | AC2 | ANa1 | ANa2
Ave Thickness [nm] | 83.97 | 89.51 | 88.22 | 87.42
Index of Refr. | 1.89 | 1.89 | 1.89 | 1.89
Wafer
xxx
003
xxx
004
xxx
002
xxx
001
n and k vs Wavelength
Will be shared
}
N-type high R wafer with PECVD deposited SiNx
For CV-measurements
Samples: